## Slide 1: First Silver Dots
10% mass loading of silver in 90% WD-40
1-3 Micron average diameter silver particles
Printed with ~12 watts of peak input power (manually controlled)

## Slide 2
< 10 micron thick Silver deposit
Al2O3 Substrate
0.75mm
0.75mm
Single pulse deposit

## Slide 3
1.5mm
1.0mm
< 10 micron thick Silver deposit
Al2O3 Substrate
Two pulse deposit
Steel needle scratch zone
Print Direction